Fixing-agent Stripper LTE-B696

Fixing-agent should be stripped before redyeing the cellulose fibre, otherwise ,it will bring different shade and uneven color.

LTE-B696 is a fixing-agent stripper and also as a masking agent. It can easily stripped the fixing-agent ,with no effect to the color and fastness

CHARACTERISTIC：

Appearance	：	yellow transparent liquid

Composition	anionic/ nonionic surfactant

pH (1% sol’n)：	7

Solubility	：	Soluble in any percent of water

FEATURES:

Stripping the fixing-agent with acid and alkali agent.

No effect on the fibre , also as a masking agent

No effect on the fastness to light.

No change on the shade, for there is no alkyl-naphthalene sulfonate

APPLICATION：

Method 1：acidic stripping

LTE-B696:  2-4 g/L

Acetic acid（pH = 4~4.5）

90℃~100℃ × 20~30 minutes  bath ratio 1:20

(2) Method 2：alkali stripping

LTE-B696:	2-4 g/L

Soda :		1 - 2 g/L

90℃~100℃ × 20~30 minutes  bath ration 1:20

sufficiently washing is needed

Remark:

the completely stripping method is first method 1 ,then method 2

if the fixing-agent is still can be stripped completely ,soda can be replaced by NaOH in method 2

ATTENTION：

This exponent based on many years experience, and the above is just as reference or direction .Sample test should be done completely before formal usage ,and we won‘t bear the imbroglio appeared because of the quality and patent.